## Slide 1: Mechanism of superconductivity in a LaAlO3-SrTiO3 heterostructure
J. Tempere1 ,S.N. Klimin1, J.T. Devreese1, D. van der Marel2
1 Theory of Quantum and Complex Systems (TQC), Universiteit Antwerpen, Belgium
2 Département de Physique de la Matière Condensee, Université de Genève, Switzerland
Theory of Quantum
and Complex systems
This work was supported by FWO-V projects G.0356.06, G.0370.09N, G.0180.09N, and G.0365.08, the WOG WO.035.04N (Belgium), the SNSF through Grant No. 200020-140761, and the National Center of Competence
in Research (NCCR) “Materials with Novel Electronic Properties–MaNEP.”

## Slide 2
Niobium-doped strontium titanate
known to geologists as tausonite
Niobium doping in SrTi1-xNbxO3 adds electrons in the t2g conduction band, resulting in an insulator-metal transition for x>0.002. For 0.005<x<0.020 it becomes superconducting with T  0.3 K
J.G. Bednorz, K.A. Muller, Rev. Mod. Phys. 60, 585 (1988), C.S. Koonce et al. Phys Rev. 163, 380 (1967).
Sr
Ti
O
SrTiO3 , with perovskite structure, is an insulating crystal with 3.25 eV bandgap
Titanium 3d
Oxygen 2p
t2g
eg
3.25 eV

## Slide 3: Experimentally detected superconductivity in bulk strontium titanate
1 C. S. Koonce et al., Phys. Rev. 163, 380 (1967).
2 G. Binnig et al., Phys. Rev. Lett. 45, 1352 (1980); A. Baratoff and G. Binnig, Physica B+C 108, 1335 (1981).
Superconductivity occurs in strontium titanate at very low temperatures T < 1 K
The critical temperature non-monotonically depends on the carrier density
Koonce et al., 1967
Baratov & Binnig, 1981

## Slide 4
Superconductivity at the LaAlO3-SrTiO3 interface
[1] A. Ohtomo, H.Y. Hwang, Nature 427, 423 (2004).
[2] N. Reyren et al., Science 317, 1196 (2007).
[3] A. Caviglia et al., Nature 456, 624 (2008).
[4] C. Richter et al., Nature 502, 528 (2013).
Doping with niobium is not the only way! At the interface between (insulating) LaAlO3 and (insulating) SrTiO3 a valence discontinuity results in a 2D electron gas[1]. This 2D layer becomes superconducting[2] at ca. 0.5 K, and Tc can be tuned by tuning the carrier density with a gate[3,4].
region 1: SrTiO3
substrate
region 3: Au gate[3,4]
or vacuum[2]
region 2: LaAlO3
layer of width l
Figures from ref. [4]

## Slide 5: LaAlO3-SrTiO3 heterostructure
Picture from: S. Thiel et al., Science 313, 1942 (2006)
1 A. Ohtomo, H. Y. Hwang, Nature 427, 423 (2004)
2 N. Nakagawa, H. Y. Hwang, D. A. Muller, Nat. Mater. 5, 204 (2006)
3 S. Thiel, G. Hammerl, A. Schmehl, C. W. Schneider, and J. Mannhart, Science 313, 1942 (2006)
High-mobility quasi 2D electron gas

## Slide 6: Experimentally detected superconductivity in the LAO-STO structure
N. Reyren, S. Thiel, A. D. Caviglia, L. F. Kourkoutis, G. Hammerl, C. Richter, C. W. Schneider, T. Kopp, A.-S. Ruetschi, D. Jaccard, M. Gabay, D. A. Muller, J.-M. Triscone, and J. Mannhart, Science 317, 1196 (2007).
BKT in superconductors:
B. I. Halperin and D. R. Nelson, J. Low Temp. Phys. 36, 599 (1979)

## Slide 7: Experimentally detected superconductivity in the LAO-STO structure
A. D. Caviglia, S. Gariglio, N. Reyren, D. Jaccard, T. Schneider, M. Gabay, S. Thiel, G. Hammerl, J. Mannhart, and J.-M. Triscone, Nature (London) 456, 624 (2008).
A modulation of the gate voltage leads to a modulation of the carrier density in the quasi two-dimensional electron gas at the interface.
As a consequence, the density-dependent critical temperature is experimentally detected.

## Slide 8: Theoretical model: multilayer structure
1
n
K
z
z0
zn-1
zn
2
zK-1
zK
z1
z2
Scheme of a multilayer structure
The coordinate z for the n-th layer lies in the range zn-1 < z < zn
ln
L
LaAlO3-SrTiO3: the asymmetric three-layer structure

## Slide 9: Optical phonons in the LaAlO3-SrTiO3 structure
Electron-phonon interaction in an asymmetric three-layer structure
Amplitudes of the electron-phonon interaction with the interface pholons in the LaAlO3-SrTiO3 heterostructure
The leading term in the electron-phonon interaction comes from the SrTiO3-like interface phonons.
The half-space phonons bring much smaller contribution
S. N. Klimin, J. Tempere, J. T. Devreese, and D. van der Marel, Phys. Rev. B 89, 184514 (2014)

## Slide 10: SrTiO3: band structure
Fermi surface of the cubic phase at 2% doping, showing the large anisotropy of the lowest band
D. van der Marel, J. L. M. van Mechelen, and I. I. Mazin, Phys. Rev. B 84, 205111 (2011)
Band dispersion of the lowest unoccupied bands of SrTiO3

## Slide 11
Tight-binding model
The ab-initio band structure of the t2g manifold is well parametrized by the following tight-binding model:
with t=35 meV, t=615 meV, D=2.2 meV, =18.8 meV
In what follows we study 4 samples, with doping
x = 0.0011, 0.0020, 0.0087, 0.0200
corresponding to, respectively:
n0 = 1.7  1019, 3.4  1019, 1.5  1020, 3.4  1020 cm-3
@ 2% doping
D. van der Marel, J.L.M. Van Mechelen, I.I. Mazin, Phys. Rev. B 84, 205111 (2011).

## Slide 12: Band splitting for the quasi 2D electron gas
In addition to the enhanced splitting of the bulk bands, the size-quantization subbands appear
S. N. Klimin, J. Tempere, J. T. Devreese, and D. van der Marel, Phys. Rev. B 89, 184514 (2014)

## Slide 13: Mechanism of superconductivity
The system
Electron subsystem
Hamiltonian
Phonons
Coulomb interaction
Electron-phonon interaction
Because the optical-phonon energies can exceed the Fermi energy, the BCS and Eliashberg approaches can be inapplicable
One-electron energy
Phonon energy
Matrix element for the electron-phonon interaction
Matrix element for the Coulomb interaction
S. N. Klimin, J. Tempere, J. T. Devreese, and D. van der Marel, Phys. Rev. B 89, 184514 (2014)

## Slide 14: Dielectric function method for superconductivity
For polar crystals with sufficiently high optical-phonon frequencies and/or low carrier densities, the conditions for the Migdal theorem are not fulfilled. Therefore we use the dielectric function method1 valid far beyond the adiabatic case.
The gap equation
contains the kernel function:
with
S. N. Klimin, J. Tempere, J. T. Devreese, and D. van der Marel, Phys. Rev. B 89, 184514 (2014)

## Slide 15: Dielectric function method for superconductivity
The effective interaction potential:
Screening is taken into account within RPA:
The non-screened potential
The acoustic-phonon contribution:
Coulomb d Electron-phonon
matrix elements
S. N. Klimin, J. Tempere, J. T. Devreese, and D. van der Marel, Phys. Rev. B 89, 184514 (2014)

## Slide 16: Kernel function and critical temperature
The kernel function is energy-nonlocal, as distinct from the BCS and Migdal-Eliashberg approaches, since it is provided by a retarded effective electron-electron interaction through the plasmon-phonon excitations.
Beyond the Migdal theorem, superconductivity in an electron-phonon system can exist despite the fact that the kernel function is positive for all energies
The critical temperature has been explicitly determined:
S. N. Klimin, J. Tempere, J. T. Devreese, and D. van der Marel, Phys. Rev. B 89, 184514 (2014)

## Slide 17: Critical temperatures: theory and experiment
The calculation, performed without fit and using parameter values known from literature, yields the critical temperatures within the same range as in the experiments.
At low densities, the critical temperature depends on the carrier density almost linearly. In this regime it is well described by a BCS-like expression with the Fermi energy instead of the Debye energy:
with l independent on the density at low densities. This is a direct consequence of the anti-adiabatic regime at low densities.
S. N. Klimin, J. Tempere, J. T. Devreese, and D. van der Marel, Phys. Rev. B 89, 184514 (2014)
N. Reyren et al., Science 317, 1196 (2007).
A. Caviglia et al., Nature 456, 624 (2008).
C. Richter et al., Nature 502, 528 (2013).

## Slide 18: Critical temperatures: theory and experiment
The calculation, performed without fit and using parameter values known from literature, yields the critical temperatures within the same range as in the experiments.
At high densities, the density dependence of the critical temperature
shows the domination of the plasmon mechanism of superconductivity.
S. N. Klimin, J. Tempere, J. T. Devreese, and D. van der Marel, Phys. Rev. B 89, 184514 (2014)
N. Reyren et al., Science 317, 1196 (2007).
A. Caviglia et al., Nature 456, 624 (2008).
C. Richter et al., Nature 502, 528 (2013).

## Slide 19: Conclusions
We have re-formulated the dielectric function method for a multilayer structure with several polar layers.
The developed technique is capable to describe superconductivity in multilayer structures with polar layers.
All phonon branches existing in the multilayer structure are taken into account.
The calculated critical temperatures lie within the same range as in the experiments without fitting.
The obtained critical temperatures support the hypothesis that the mechanism of superconductivity in the LaAlO3-SrTiO3 structures is provided by the electron - optical-phonon interaction.